IAWA Journal - Volume 25(3)

| Author(s): | Lloyd A. Donaldson; Jenny Grace; Geoff M. Downes |
| --- | --- |
| Title: | WITHIN-TREE VARIATION IN ANATOMICAL PROPERTIES OF COMPRESSION WOOD IN RADIATA PINE |
| Source: | IAWA Journal, Volume 25, Issue 3 |
| Publication Year: | 2004 |
| Pages: | 253-271 |
| Keywords: | lignin distribution; Compression wood; Pinus radiata; basic density; anatomical properties; microfibril angle; cell dimensions |
| Abstract: | Two trees of radiata pine, one showing severe lean, the other growing almost vertically, were assessed for the presence and anatomical properties of compression wood, including anatomy, lignin distribution, microfibril angle, basic density, radial and tangential lumen diameter and cell wall thickness. Both trees contained significant amounts of compression wood although the severity and amount of compression wood was greater in the leaning tree. Changes in lignin distribution seem to be characteristic of the mildest forms of compression wood with reduced lignification of the middle lamella representing the earliest change observed from normal wood. An increase in microfibril angle was associated with both mild and severe compression wood although examples of severe compression wood with the same or smaller microfibril angles than opposite wood, or with very small microfibril angles, were found. When segregated into mild and severe compression wood the average difference in microfibril angle was 4° and 8° respectively compared with opposite wood. Within-ring distribution of microfibril angle was different in severe compression wood compared to opposite wood with higher angles in the latewood.Severe compression wood showed a 22% increase in basic density compared to mild compression wood and opposite wood. The increased density was accounted for in terms of a 26% increase in tracheid wall thickness throughout the growth ring, offset by a 9% increase in radial lumen diameter, slightly greater in the latewood. There were no significant changes in density or cell dimensions in mild compression wood compared with opposite wood. |
| DOI: | 10.1163/22941932-90000364 |

| Author(s): | K.M. Bhat; P.B. Priya |
| --- | --- |
| Title: | INFLUENCE OF PROVENANCE VARIATION ON WOOD PROPERTIES OF TEAK FROM THE WESTERN GHAT REGION IN INDIA |
| Source: | IAWA Journal, Volume 25, Issue 3 |
| Publication Year: | 2004 |
| Pages: | 273-282 |
| Keywords: | wood anatomy; Tectona grandis; ring-porous tropical hardwood; growth rate; mechanical properties |
| Abstract: | The three major teak provenances of the Western Ghats in India were characterised in terms of mechanical and anatomical wood properties. Within the same age of 21-year-old plantations, teak from the North Kanara provenance, generally known to display slow growth, had the lower values of static bending (modulus of rupture and modulus of elasticity) and longitudinal compressive stresses than the Malabar provenance (Nilambur). The weaker timber of North Kanara provenance was attributed to its relatively high percentage of parenchyma and low percentage of fibres in the narrower rings, probably as an adaptation to nutrient-rich soil condition. Observations of 65-year-old plantations reveal that there was a trend for bending stiffness (modulus of elasticity) and maximum stress (modulus of rupture) of the timber to be highest towards the southernmost geographic location (Konni) within the latitudinal range of 9° to15° S with a greater percentage of cell wall (with higher lignification) despite the slower growth rate and well defined ring-porosity with wider bands of earlywood parenchyma tissue. The study thus underlines the need to recognise the provenance source of variation to explain the varied growth-structure-property relationships of teak and to utilise the Indian genetic resources to the optimum in future teak improvement programmes. |
| DOI: | 10.1163/22941932-90000365 |

| Author(s): | Yoko Watanabe; Yasuo Kojima; Toshihiro Ona; Takayuki Asada; Yuzou Sano; Kazumi Fukazawa; Ryo Funada |
| --- | --- |
| Title: | HISTOCHEMICAL STUDY ON HETEROGENEITY OF LIGNIN IN EUCALYPTUS SPECIES II. THE DISTRIBUTION OF LIGNINS AND POLYPHENOLS IN THE WALLS OF VARIOUS CELL TYPES |
| Source: | IAWA Journal, Volume 25, Issue 3 |
| Publication Year: | 2004 |
| Pages: | 283-295 |
| Keywords: | UV microspectrophotometry; Eucalyptus globulus; lignin; Eucalyptus camaldulensis; cell walls; polyphenol; histochemistry |
| Abstract: | We examined the effects of polyphenols on the analysis of lignin by histochemical methods, namely, the Mäule color reaction coupled with microspectrophotometry and ultraviolet microspectrophotometry, in wood of Eucalyptus camaldulensis and E. globulus. Thin sections and wood meals were extracted with solutions of alkali at different concentrations. The amounts of alkali-soluble extractives increased with increasing concentrations of NaOH. By contrast, there was no clear correlation between amounts of Klason lignin and the concentration of NaOH. The visible-light absorption spectra of cell walls of all woody tissues from both species changed after alkali extraction. In particular, the spectra of cell walls of vessel elements changed considerably, even when only a dilute solution of alkali was used. Ultraviolet absorption spectra did not show clear changes after extraction with alkali. These results indicate that polyphenols in cell walls affect the results of histochemical analysis. Therefore, a preliminary extraction with alkali, namely, extraction with a 1% solution of NaOH, is needed to assess the precise distribution of lignins in the cell walls of Eucalyptus wood by histochemical methods. The cell walls of wood fibers of Eucalyptus camaldulensis contained both guaiacyl and syringyl units and those of vessel walls contained mostly guaiacyl units. However, the cell walls of wood fibers in Eucalyptus globulus contained mainly syringyl units, while those of vessel elements contained both guaiacyl and syringyl units. Syringyl-type polyphenols, which have spectra similar to those of syringyl-type lignins, were found in the cell walls of wood fibers and vessel elements and in cell corners among wood fibers in both species of Eucalyptus. |
| DOI: | 10.1163/22941932-90000366 |

| Author(s): | Ling-Long Kuo-Huang; Yan-San Huang; Shin-Shin Chen; Yi-Ru Huang |
| --- | --- |
| Title: | GROWTH STRESSES AND RELATED ANATOMICAL CHARACTERISTICS IN COCONUT PALM TREES |
| Source: | IAWA Journal, Volume 25, Issue 3 |
| Publication Year: | 2004 |
| Pages: | 297-310 |
| Keywords: | growth strain; microfibril angle; vascular bundles; Cocos nucifera; fibers; growth stress |
| Abstract: | The surface growth strains and the distribution of internal stresses in woody palms, coconut (Cocos nucifera L.), were determined by measuring the strains released by the kerf method using strain gauges. Measurements of the surface strains showed that longitudinal tensile stresses existed at the cortex, while longitudinal compressive stresses existed at the periphery of the central cylinder. These stresses may be generated from the fibers located in the scattered fiber and vascular bundles. In the central cylinder of narrow and wide trunks, both positive and negative stresses were observed, indicating the existence of some tensile and compressive stresses in the trunks. The amount of stress varied from base to top and from periphery to core because of the variation in proportion of the vascular bundles and the fibers, and the cell wall layers of fibers along these points. Furthermore, changes in the angle of vascular bundles and of the fiber microfibrils were correlated with the various tensile and compressive stresses located in the central cylinder of the trunks. |
| DOI: | 10.1163/22941932-90000367 |

| Author(s): | Mattias K. Moëll; Minoru Fujita |
| --- | --- |
| Title: | FOURIER TRANSFORM METHODS IN IMAGE ANALYSIS OF COMPRESSION WOOD AT THE CELLULAR LEVEL |
| Source: | IAWA Journal, Volume 25, Issue 3 |
| Publication Year: | 2004 |
| Pages: | 311-324 |
| Keywords: | lumen shape; Picea sitchensis; Pinus radiata; tracheid shape; Image analysis; fast Fourier transform |
| Abstract: | Compression wood affects the overall quality of construction timber and paper quality. We have investigated the microscopic features of lumen shape and tracheid shape for compression wood studies and detection in softwoods. In this paper, we describe a method for directly analyzing tracheid and lumen shape over an entire image. The method uses the Fast Fourier Transform (FFT) and reduces the two-dimensional image data to one-dimensional data, from which lumen and tracheid shape can be evaluated. We illustrate the method by comparison of compression wood images to normal wood images. The results of detecting severe compression wood were successful, while the detection of weak compression wood was not satisfactory. |
| DOI: | 10.1163/22941932-90000368 |

| Author(s): | José Graça; Helena Pereira |
| --- | --- |
| Title: | THE PERIDERM DEVELOPMENT IN QUERCUS SUBER |
| Source: | IAWA Journal, Volume 25, Issue 3 |
| Publication Year: | 2004 |
| Pages: | 325-335 |
| Keywords: | lenticels.; epidermis; Quercus suber; phellem; cork; phellogen |
| Abstract: | In the cork oak (Quercus suber L.), the phellogen differentiates during the first year of growth in the cell layer immediately under the epidermis and divides to form 3–6 suberized phellem cells. Division of the phellogen only occurs after suberization of the previous divided cell. During the first four years of growth, the phellem cells have tannin-filled lumens and it is only in the 5th to 7th years that they acquire the characteristics of ʻadultʼ cork cells with empty lumens and thin suberized walls. The lenticels are formed by the lenticular phellogen, which differentiates under the stomata and has a high meristematic activity. In this region, the cells are unsuberized, with a loose arrangement and intercellular voids, constituting the filling or complementary tissue. After three years, the lenticels appear as small protuberances that soon become conspicuous. Inclusions of sclerenchymatous nodules and isolated sclereids occur occasionally mostly in the vicinity of, or in, the lenticels. |
| DOI: | 10.1163/22941932-90000369 |

| Author(s): | Sheng Du; Hiroki Uno; Fukuju Yamamoto |
| --- | --- |
| Title: | ROLES OF AUXIN AND GIBBERELLIN IN GRAVITY-INDUCED TENSION WOOD FORMATION IN AESCULUS TURBINATA SEEDLINGS |
| Source: | IAWA Journal, Volume 25, Issue 3 |
| Publication Year: | 2004 |
| Pages: | 337-347 |
| Keywords: | auxin; MBOA (6-methoxy-2-benzoxazolinone); tension wood; Aesculus turbinata; raphanusanin; gibberellin; NPA (N-1-naphthylphthalamic acid); uniconazole-P. |
| Abstract: | The lowest nodes of 6-week-old Aesculus turbinata seedlings were treated with uniconazole-P, an inhibitor of gibberellin (GA) biosynthesis, or a mixture of uniconazole-P and GA3 in acetone solution. To the seedling stems, an inhibitor of auxin transport (NPA) or inhibitors of auxin action (raphanusanin or MBOA) were applied in lanolin paste. The seedlings were tilted at a 45° angle and kept for 10 weeks before histological analysis. Decreases in both normal and tension wood formation followed the application of uniconazole-P. The application of GA3 together with uniconazole-P partially negated the effect of uniconazole-P alone. The application of NPA inhibited tension wood formation at, above, and below the lanolin-treated portions. The treatment of raphanusanin or MBOA also resulted in decreases in tension wood formation at the treated portions. The inhibitory effects of these chemicals applied on the upper side of tilted stems or around the entire stem were greater than on the lower side. The application of uniconazole-P in combination with raphanusanin, MBOA or NPA showed synergistic effects on the inhibition of tension wood formation. The results suggest that both auxin and GA regulate the quantitative production of tension wood fibers and are essential to tension wood formation. |
| DOI: | 10.1163/22941932-90000370 |

| Author(s): | Sidney R. Ash; Rodney A. Savidge |
| --- | --- |
| Title: | THE BARK OF THE LATE TRIASSIC ARAUCARIOXYLON ARIZONICUM TREE FROM PETRIFIED FOREST NATIONAL PARK, ARIZONA |
| Source: | IAWA Journal, Volume 25, Issue 3 |
| Publication Year: | 2004 |
| Pages: | 349-368 |
| Keywords: | phloem; bark; periderm; Late Triassic; Araucarioxylon arizonicum; rhytidome; phytophagous insects; cambium |
| Abstract: | This paper contains a description of the only known non-banded bark in the geologic record. The bark is attached to a branch of the Araucarioxylon arizonicum tree that was found recently in the Late Triassic Chinle Formation (~ 220 Mya) in Arizona. In the fossil the vascular cylinder is almost totally enclosed in rough bark 2–11 mm in thickness. The inner bark is less than 1 mm thick and comprises a very narrow zone of presumed phloem containing infrequent fibers. The outer bark varies in thickness up to 10 mm, and consists of curving lenses of sequent periderm free of both dilation tissue and resin canals but is quite unlike the banded bark of Araucaria heterophylla. Wide zones of very thin-walled rectangular parenchyma cells arranged in radial files and groups of thin-walled spongy parenchyma, and small clusters as well as solitary sclerenchyma occur in the rhytidome. The vascular cambium contains 1–4 fusiform cells per radial file. Uniseriate rays are common in the secondary xylem and extend to the cambial zone. Small (1 mm in diameter), simple tunnels in the bark and wood indicate that the branch was attacked by phytophagous insects. A possible petrified beetle larva similar in form and size to Anobium is associated with these tunnels. |
| DOI: | 10.1163/22941932-90000371 |

| Author(s): | Jakub Sakala; Catherine Privé-Gill |
| --- | --- |
| Title: | OLIGOCENE ANGIOSPERM WOODS FROM NORTHWESTERN BOHEMIA, CZECH REPUBLIC |
| Source: | IAWA Journal, Volume 25, Issue 3 |
| Publication Year: | 2004 |
| Pages: | 369-380 |
| Keywords: | Czech Republic; Liquidambaroxylon; Oligocene; modern wood.; Cercidiphyllaceae; fossil wood; Cercidiphylloxylon; Hamamelidaceae |
| Abstract: | Two species of fossil angiosperm wood are described from the Oligocene of northwestern Bohemia in the Czech Republic. One specimen from Kadan–Zadní vrch Hill is identified as Cercidiphylloxylon kadanense Prakash et al. Because of its superior preservation, the specimen is designated as an epitype to the original holotype specimen of the species and genus. Cercidiphylloxylon kadanense is known only from the locality of Kadan–Zadní vrch Hill, and it represents the oldest fossil wood of true Cercidiphyllum Sieb. & Zucc. Three other wood specimens from Zichov are attributed to Liquidambaroxylon speciosum Felix. Modern wood of some species of Cercidiphyllum Sieb. & Zucc., Liquidambar L., Altingia Noronha, Corylopsis Sieb. & Zucc., Distylium Sieb. & Zucc., and Hamamelis L. was examined to determine how to distinguish the wood of Cercidiphyllum (Cercidiphyllaceae) from similar woods of Hamamelidaceae. The number of bars in the scalariform perforation plates of the vessels is about 40 in Cercidiphyllum, and about 20 in the Hamamelidaceae. Rays are variable, even at intra-specific level, and are not suitable for distinguishing these woods. These criteria were found to be useful in evaluating affinities of the fossil woods. |
| DOI: | 10.1163/22941932-90000372 |